## Slide 1: FUNCTIONAL PROPERTIES OF ACID-THINNED SOURSOP STARCH (Annona muricata) .
by
Oderinde, A. A., Oguntade, B. K., Adebona F. O., Jimoh H. A.
The Federal Polytechnic, Ilaro, Ogun State, Nigeria

## Slide 2: PRESENTATION OUTLINE

## Slide 3
INTRODUCTION
      Background information
      Statement of problem
      Significance of the research
      Aim and Objectives of the research
      Scope of the study

## Slide 4
    PRESENTATION OUTLINE Cont’d
  MATERIALS AND METHODS
      Sample Collection and Treatment
      Procedures
  RESULTS AND DISCUSSIONS
  CONCLUSIONS
  SELECTED REFERENCES

## Slide 5
INTRODUCTION

## Slide 6
Background Information
    Starch abundance and versatility.
STARCH USE
FOOD
NON-FOOD
Canning
Frozen Foods
Confectionary
Dairy products
Textile
Paper
Cosmetics/Pharm
Adhesives

## Slide 7
The problem
    Limitations in native form
    Over-dependence on conventional sources
Significance of this work
    Overcoming native starch limitations by modification
    Breaking new grounds to augment existing ones

## Slide 8
PHYSICAL
CHEMICAL
BIOTECH
Use of temperature/moisture combinations, pressure, shear, irradiation and mechanical attrition to alter the physical size of starch granules
PHYSICAL
CHEMICAL
BIOTECH
STARCH MODIFICATION
Introducing desirable alterations in the starch structure by glycosidic bond cleavage, forming new functional groups, substitution of free available hydroxyl groups or bridging of molecular chains
Biotechnological modifications are mostly achieved during the growth of the plant to produce starches with different amylose/amylopectin levels, phosphorus contents, etc or by enzymatic activities of single or multiple enzymes

## Slide 9
Unconventional Starch source
    Soursop (Annona muricata)

## Slide 10
AIM OF STUDY

## Slide 11
The aim of this work is to isolate starch from a lesser-known source and enhance its properties through modification.

## Slide 12
OBJECTIVES

## Slide 13
The objectives of this work are to:
    Isolate starch from soursop mesocarp;
    Modify the isolated starch by acid-thinning;
    Determine the physicochemical and functional
    properties of native and modified soursop starches.

## Slide 14
MATERIALS AND METHODS

## Slide 15
Sample Collection and Treatment
Isolation and Purification of Starches (Lawal, 2004)

## Slide 16
  Functional properties
      Swelling power and solubility
      Oil and water absorption capacities
      Gelation
      Bulk and tapped densities
      Light transmittance
      Pasting properties

## Slide 17
STATISTICAL ANALYSIS
Analyses were done in triplicate. Analysis of variance was performed to calculate significant differences in treatment means and LSD (P < 0.05) was used to separate means (SigmaPlot 12.0).

## Slide 18
RESULTS AND DISCUSSIONS

## Slide 19
Chart: Fig.1. Effect of temperature on native and acid-thinned soursop starches. Error bars: Standard deviations Results are means of triplicate determinations Ns, native starch; At, acid-thinned starch.
| 55 | 65 | 75 | 85 | 95
Ns | 420 | 950 | 1180 | 2150 | 2630
At | 480 | 880 | 1140 | 1420 | 2290

## Slide 20
Chart: Fig. 2. Effect of temperature on solubilty of native and acid-thinned soursop starches. Error bars: Standard deviations Results are means of triplicate determinations Ns, native starch; AT, acid-thinned starch.
| 55 | 65 | 75 | 85 | 95
NS | 20 | 27 | 30 | 39 | 43
AT | 30 | 25 | 29 | 36 | 40

## Slide 21
Chart: Fig. 3. Effect of pH on swelling power of native and acid-thinned soursop starches. Error bars: Standard deviations Results are means of triplicate determinations Ns, native starch; AC, acetylated starch.
| 2 | 4 | 6 | 8 | 10 | 12
NS | 20 | 20.25 | 29 | 34.65 | 46 | 53.6
AT | 19.23 | 20.13 | 25.9 | 31.2 | 41.25 | 48.76

## Slide 22
Chart: Fig. 2. Effect of pH on solubility of native and acid-thinned soursop starches. Error bars: Standard deviations Results are means of triplicate determinations Ns, Native starch; AT, acid-thinned starch.
| 2 | 4 | 6 | 8 | 10 | 12
NS | 18 | 20 | 23 | 32 | 37 | 40
AT | 20 | 26 | 35 | 41 | 47 | 53

## Slide 23
Chart: Fig. 5. Water and Oil absorption capacity of native and acid-thinned soursop starches. Error bars: Standard deviations Results are means of triplicate determinations. NS, native starch; AT, acid-thinned starch.
| NS | AT
WAC | 0.9 | 0.35
OAC | 0.74 | 1.01

## Slide 24
Chart: Fig. 6. Bulk and tapped density of native and acid-thinned starches. Errors bars: standard deviation. Results are means of triplicate determinations. NS: native starch; AT: acid-thinned starch.
| Bulk Density | Tapped Density
NS | 0.43 | 0.5
AT | 0.45 | 0.52

## Slide 25
Table 1. Pasting Properties of Native and Acid-Thinned Soursop Starches. |  |  |  |  |  |  | 
Sample | Peak Viscosity | Trough | Breakdown | Final Viscosity | Set back | Peak time | Pasting temperature
Native | 6992.00 | 2944.00 | 4048.00 | 4048.00 | 1120.00 | 6.93 | 84.10
Acid-Thinned | 395.50 | 20.50 | 375.00 | 59.50 | 39.00 | 4.44 | 82.85

## Slide 26
Table 3. Gelation properties of Native and Acid-Thinned soursop starches. |  | 
Concentration (%w/v) | Starch Sample | 
 | Native | Acid Thinned
2 | -Liquid | -Liquid
4 | -Liquid | -Liquid
6 | -Liquid | -Viscous
8 | -Viscous | +Gel
10 | -Viscous | +Gel
12 | +Gel | +Gel
14 | +Gel | +Firm gel
LGCa | 12 | 8

## Slide 27
CONCLUSIONS

## Slide 28
  Acid-thinning increased soursop swelling capacity and solubility with increased temperature and pH;
  Acid-thinning increased oil absorption capacity of soursop starch;

## Slide 29
  Gelation property of the starch also improved
  The pasting temperature of modified starch was reduced.

## Slide 30
Selected References
Karmakar, R., Ban, D., and Ghosh, U., (2014). Comparative study of native and modified starches isolated from conventional and non-conventional sources. Journal of international food research, 21(2), 597-602.
Kolawole, S., Igwemmar, N., and Bello, H., (2013). Comparison of the physiochemical properties of starch from Ginger (Zingiber officinale) and Maize (Zea mays). Journal of International science and research, 2, 2319-7064.
Lawal, O. S., (2004). Composition, physicochemical properties and retrogradation characteristics of native, oxidised, acetylated and acid-thinned new cocoyam (Xanthosoma sagittifolium) starch. Food Chemistry 87, 205–218.
Nwokocha, L., and Williams, P., (2009). New Starches: Physiochemical properties of sweetsop (Annona squamosal) and soursop ( Annona muricata) starches, Carbohydrate polymer, 78(3), 462-468.
Wang, L., & Wang, Y. (2001). Structures and physicochemical properties of acid- thinned corn, potato and rice starches. Starch, 53, 570–576.
Zhang, H., Zhou, X., He, J., Wang, T., Luo, X., Wang, R., … Chen, Z., (2017). Impact of amylosucrase modification on the structural and physiochemical properties of native and acid-thinned waxy corn starch. Journal of food chemistry, 220, 413- 419.

## Slide 31: THANK YOU FOR LISTENING