## Slide 1: A comparative physicochemical study of two β-substituted octa pyridyloxy and pyridylsulfanyl indium phthalocyanine
By
Osifeko, Olawale Lawrence
and
Prof. T. Nyokong

## Slide 2: Introduction
Phthalocyanines are a family of aromatic macrocycles based on an extensive delocalized 18-π electron system.
The solubility of phthalocyanines can be enhanced by adding different kinds of substituents such as
long chain alkyl,
crown ether, Organic solvents
alkylthio or alkoxy groups
sulfonates group
Carboxyl group Aqueous Media
Ammonium group
Notes: The common means for preparing water soluble Pcs with high efficiency is to attach hydrophilic groups like polyethylene glycol, amino acid, carbohydrates [13-15], ionic groups including cationic and anionic substituent [16-18] at the peripheral and axial positions of Pc ring.

## Slide 3: SITE OF MODIFICATION
Non-peripheral
or
α substitution
Variation of the metal
Axial substitution
Peripheral
or
β substitution
Notes: Synthesis, characterization and investigation of the photophysical and photochemical properties of highly soluble novel metal-free, zinc(II), and indium(III) phthalocyanines substituted with 2,3,6-trimethylphenoxy moieties

## Slide 4: Properties of Photosensitiser
A good photosensitizer absorb photons efficiently and have
  high absorption coefficient
  high quantum yield of triplet formation
  the triplet state should be long lived
  Ability of being activated by red light or near infra red light
  Solubility potential in aqueous media

## Slide 5
APPLICATIONS OF PHTHALOCYANINES

## Slide 6: AIM
To design effective water soluble metallophthalocyanines for inactivating bacteria in water (PACT)
Synthesis and Characterisation of metallophthalocyanines and its quaternized form

## Slide 7: Photodynamic Antimicrobial Chemotherapy
PS
3O2
1O2
PS*
Light Source
Light Source
PACT is based on 3 concepts
a non-toxic photosensitizer,
visible light of appropriate wavelength
Molecular oxygen

## Slide 8
Incubation with
photosensitizer
P
Accumulation of
Photosensitizer
P
MECHANISM OF DESTRUCTIVE ACTION OF
PHOTOSENSITIZATION IN THE CELL
Irradiation
P1
Light
Cell Death

## Slide 9: SYNTHESIS & CHARACTERIZATION

## Slide 11: ELECTRONIC ABSORPTION SPECTRAL
Chart: Wavelength (nm)
Chart: Wavelength (nm)
= absorption
= excitation
= emission
= In(pyS)8 Pc DMSO
= Qrt In(pyS)8 Pc DMSO
= Qrt In(pyS)8 Pc H2O
= Qrt In(pyS)8 Pc H2O-Trit X
Notes: the absorption spec- tra of conjugate ZnPc-PL was characterized by a Soret band maximum at 344 nm and a Q-band at 680 nm, while Ce6-PL [16] has a Q-band at 663 nm and a Soret band maximum at 406 nm (as shown in Fig. 1), indicating that the lysine conjugation does not affect the chemical and photochemical properties of ZnPc, as previously observed in the conjugate of ZnPc modified with five lysines [1
The UV-vis spectral of the complexes gave a characteristic strong Q and Soret band in DMSO and aqueous media for the cationic complexes (fig. 1) in DMSO, the complexes show a bathochromic shift of

## Slide 12
Chart: Wavelength (nm)
In(pyO)8 | EXPECTED | FOUND
C (%) | 61.44 | 59.53
H (%) | 2.86 | 3.04
N (%) | 15.92 | 14.64
In(pyS)8 | EXPECTED | FOUND
C (%) | 56.30 | 55.56
H (%) | 2.62 | 2.88
N (%) | 14.59 | 14.87

## Slide 13
In(pyS)8 Pc
MALDI TOF MS m/z:
Calcd: 1535
1504.997
1540.565
In(pyO)8 Pc
MALDI TOF MS m/z:
Calcd: 1407
1411.795

## Slide 15
Singlet Oxygen Quantum Yield
Chart: Qrt In(pyS)8 Pc + Tri-X
Chart: In(pyO)8 Pc
Ф∆ = 0.46
ФPd = 6.34 X 10-7
Ф∆ = 0.21
ФPd = 7.00 X 10-6
Singlet oxygen quantum yield () =
Number of molecules in the triplet state/ quanta of light absorbed
Values 0-1
DPBF = 1,3 diphenylisobenzofuran
ADMA= anthracene-9,10-bis-methylmalonate
0 min
120 min
ADMA

## Slide 16
Phosphoresence
Fluoresence
Excited Singlet
state
Triplet state
JABLONSKI DIAGRAM
Singlet oxygen
ФIC
ФT
ФF
ISC
Bacteria death
Bacterial

## Slide 17: Transient curve and Triplet Decay curve in DMSO
Chart: In(pyS)8 Pc
| 400 | 410 | 420 | 430 | 440 | 450 | 455 | 460 | 465 | 470 | 475 | 480 | 485 | 490 | 492 | 494 | 496 | 498 | 500 | 510 | 520 | 530 | 540 | 550 | 560 | 570 | 580 | 590 | 600 | 605 | 610 | 620 | 630 | 640 | 642 | 645 | 650 | 660 | 665 | 670 | 680 | 682 | 690 | 700 | 705 | 710 | 715 | 720 | 730 | 740 | 750 | 760 | 770 | 780 | 790 | 800
 | 0.0096754 | 0.00083744 | 0.0042216 | 0.0041911 | 0.0048735 | 0.0049088 | 0.0047544 | 0.0046052 | 0.0050677 | 0.0057092 | 0.0058661 | 0.0061475 | 0.0053254 | 0.0066084 | 0.0072887 | 0.0070829 | 0.0069626 | 0.0057869 | 0.0055961 | 0.0074544 | 0.0073147 | 0.0078227 | 0.0078609 | 0.0079138 | 0.008309 | 0.0085945 | 0.0083322 | 0.0067888 | 0.0064928 | 0.0062584 | 0.0060388 | 0.0058194 | 0.0054063 | 0.0020726 | 0.0012535 | -0.00084046 | -0.0020646 | -0.0013256 | -0.00053134 | -0.00053629 | -0.00047692 | -0.0010904 | -0.0020577 | -0.0048302 | -0.0080624 | -0.015292 | -0.027029 | -0.032045 | -0.034808 | -0.01882 | -0.0056511 | -0.0016519 | -0.0017781 | -0.002282 | -0.0030076 | -0.0025871
ФT = 0.57
τT = 61 (µS)

## Slide 18: EXPERIMENTAL DATA
Comp | aλabs (nm) | aλemm (nm) | aλexc (nm) | ФF | F (ns) | ФT | Ф∆ | ФIC | τT (µS) | Фpd 10-6 | S∆
3 | 717 | 731 | 721 | 0.011 | 0.23 | 0.57 | 0.45 | 0.42 | 61 | 1.70 | 0.79
4 | 714 710b | 730 728b | 723 722b | 0.012 0.02b | 0.23 0.28b |  | 0.33 0.21b |  |  | 64.1 7.00b | 0.51 -
5 | 698 | 716 | 705 | 0.012 | 0.25 | 0.53 | 0.46 | 0.46 | 56 | 0.63 | 0.66
6 | 699 697b | 711 710b | 703 702b | 0.013 0.018b | 0.33 0.33b | 0.48 - | 0.33 0.31b | 0.51 - | 66 - | 1.88 13.20b | 0.51 -

## Slide 19
Chart: In(pyO)8 Pc

## Slide 20: Conclusion
We were able to successfully synthesis and characterised the photosensitisers
We have established that the pyridylsulfanyl moiety is more stable than the pyridyloxy moiety
We observed that pyridyloxy moiety easily form radical but do not transform or degrade to other components
We affirm that pyridysulfanyl moiety is a better photosensitiser than pyridyloxy moeity

## Slide 21: Acknowledgements
Prof. T. Nyokong
Dr J. Mack
Dr J. Britton
Ms. Gail
S22 family
Chemistry department

## Slide 23
THANK YOU